
ATR-FTIR analysis on aliphatic hydrocarbon bond (C-H) formation and carboxyl content during the ageing of DC air plasma treated cotton cellulose and its impact on hydrophilicity 
S.Anitha*, K.Vaideki

S.Anitha*, Department of Physics, PSG Polytechnic College, Coimbatore, India. K.Vaideki, Department of Applied Science, PSG College of Technology, Coimbatore, India.
Email : vp.anitha@gmail.com, Phone no: 0422-2572177
[image: image1.png]DC-BT

T L} T v L L L} L) Ll
3600 3400 3200 3000 3600 3500 3400 3300 3200 3100 3000
DC-BT DC-AT

T v T v T T T T
3000 2950 2900 2850 2800

DC-AT

1760 1750 1740 1730 1720 1710 1700 1760 1740 1720 1700




Fig. 1 Schematic diagram of DC plasma chamber
[image: image6.png]------- Intramolecular hydrogen bonding
------- Intermolecular hydrogen bonding

Glycosidic linkage




Figure 2 ATR-FTIR spectra of control and DC air plasma 
(optimised process parameters) treated sample
[image: image12.jpg]Needlevalve  Process gas

K K / Ground

2em

+Ve

23 cm

Power supply

Rotary vacuum pump





Figure 3 Deconvoluted spectra of control and DC air plasma 
(optimised process parameters) treated sample
[image: image2.png]Intensity (a.u)

N
2 Control
DC plasma
|§§
o

A\ g

I J I J I J I

20 40 60 80

20 (degrees)




   [image: image3.png]1.03nm

A CHgrowp @ OH group
_O- oxygen @~ CH,0H





[image: image7.emf]
[image: image8.png]EHT = 3.00 kV

EHT = 3.00 kv
WD =134 mm

EHT = 3.00 kV
WD =134 mm

Control

Signal A = SE2
Mag = 0

Signal A = SE2
Mag = 500X

Signal A = SE2
Mag= 1.00KX

Signal A = SE2
Mag= 5.00KX

Signal A = SE2
Mag = 20.00 KX

DC air plasma

- e

EHT = 3.00 kv Signal A= SE2
WD = 7.3 mm Mag= 250X

EHT = 3.00 kv Signal A = SE2
WD = 7.3 mm Mag= 500

EHT = 3.00 kv Signal A= 3SE2
WD = 72mm Mag= 1.00KX

EHT = 5.00 kV Signal A =SE2
WD = 7.2mm Mag= 5.11KX

EHT = 5.00 kv Signal A = SE2
WD = 7.2mm Mag = 20.00 KX





Figure 4 X-ray diffractogram of control and DC air plasma 
(optimised process parameters) treated sample
[image: image9.png]



Figure 5 Structural changes due to DC air plasma treatment using optimised process parameters
[image: image10.png](002)
/

N

(T01)





Figure 6 FESEM micrographs of control and DC air plasma 
(optimised process parameters) treated fabric
[image: image11.png]Control
—— DC plasma

absorbance

-1t v 1 ' 1 - 11 1
4000 3500 3000 2500 2000 1500 1000 500
wavenumber (cm™1)



 
Figure 7 Deconvolution of C=O peaks for DC air plasma treated sample 
[image: image4.png]Absorbance

0.004

0.003 —

0.000 —

3 v Control
- i o DC Plasma (on the day)
v, i & DCPlasma (1 week)
v i+ DC Plasma (1 month)
Y *

3000

2950

2000 2850 2800 2750
wave number (cm™)

2700




Figure 8 Ageing analysis with reference to the concentration of ring CH[image: image5.png]


















1

