ATR-FTIR analysis on aliphatic hydrocarbon bond (C-H) formation and carboxyl content during the ageing of DC air plasma treated cotton cellulose and its impact on hydrophilicity

S.Anitha*, K.Vaideki

S.Anitha*, Department of Physics, PSG Polytechnic College, Coimbatore, India. K.Vaideki, Department of Applied Science, PSG College of Technology, Coimbatore, India.

Email : vp.anitha@gmail.com, Phone no: 0422-2572177

Table 1 IR frequency of control and DC air plasma treated sample

| Wavenumber (cm-1) Literature | Wavenumber (cm-1) Control fabric | Wavenumber (cm-1) DC plasma treated fabric | Interpretation |
| --- | --- | --- | --- |
| 3455–3410 (3420) | 3456 | 3454 | O2H···O6 intramolecular hydrogen bond in cellulose |
| 3375–3340 | 3335 | 3339 | O3H···O5 intramolecular hydrogen bond in cellulose |
| 3310-3230 | 3255 | 3273 | O6H···O3 intermolecular hydrogen bond in cellulose |
| 2981-2933 | 2952 | - | Asymmetric CH2 valence vibration |
| 2940-2850 | 2898 2870 | 2901 2874 | Symmetric CH2 valence vibration |
| 2980-2835 | 2918 2853 | 2925 2856 | Ring CH, CH2,CH2OH in cellulose from C6 |
| 1738–1709 | 1741 1728 1720 1710 | 1742 1730 1720 1712 | C=O stretch in unconjugated ketones, carbonyls, esters. |
| 1685–1655 | 1655 | 1655 | C=O stretch |
| 1636 | 1638 | 1638 | Adsorbed water |
| 1594 and 1558 | - | 1599 | C=O stretch |
| 1435 | - | 1431 | H–O–C bending |
| 1430–1416 (1420) | 1425 | 1431 | CH2 scissoring at C(6) in cellulose |
| 1376–1372 (1374) | 1370 | 1370 | C–H deformation in cellulose |
| 1364 | 1364 | 1364 | Symmetric C–H bending |
| 1338–1335 | 1336 | 1338 | O–H in-plain deformation |
| 1316 | 1315 | 1316 | CH2 wagging |
| 1282–1277 | 1261 | 1261 | C–H deformation |
| 1235–1225 | 1236 | 1237 | O–H in-plain deformation at C(6) |
| 1205–1200 | 1201 | 1202 | O–H in-plain deformation |
| 1162–1125 (1159) | 1159 | 1159 | C–O–C asymmetric from -glycosidic link in cellulose |
| 1110 | 1110 | 1110 | Ring asymmetric valence vibration |
| 1060–1015 (1170) | 1053 | 1053 | C–O vibration mainly from C(3)···O(3)H in cellulose II |
| 1035–1030 | 1027 | 1027 | C–O stretching |
| 996–985 | 997 | 997 | C–O valence vibration at C(6) |
| 896–892 (899) | 895 | 895 | C–O–C valence vibration of -glycosidic link |
| 670–668 | 665 | 665 | O–H out-of-plane bending |

Table 2 Hydrogen bond energy, LOI, TCI, HBI and intensity of acid groups of DC air plasma 
(optimised process parameters) treated sample

| Bond energy and Bond length |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Process Parameters |  |  |  |  | Intermolecular O6H···O3 |  |  |  |  |  |  | Intramolecular O3H···O5 |  |  |  |  | Intramolecular O2H···O6 |  |  | Intersheet hydrogen bond (C – H···O) |  |  |  | Intersheet hydrogen bond (C – H···O) |  |  |
| P | I |  | t |  | (3230-3310) |  |  |  |  |  |  | (3340-3375) |  |  |  |  | (3405-3460) |  |  | 2920 |  |  |  | 2850 |  |  |
|  |  |  |  |  | BL (Å) |  | EH (kJ) |  |  |  |  | BL (Å) |  | EH (kJ) |  |  | BL (Å) |  | EH (kJ) | BL (Å) |  | EH (kJ) |  | BL (Å) |  | EH (kJ) |
| 0.5 | 25 |  | 15 |  | -0.0041 |  |  | 1.2945 |  |  |  | -0.2877 |  | 0.0719 |  |  | 0.0005 |  | -0.1438 | -0.0016 |  | 0.5034 |  | -0.0007 |  | 0.2158 |
| TCI, LOI and HBI |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Process Parameters |  |  |  | IR Crystallinity Ratio |  |  |  |  |  |  |  |  |  | Lateral order index |  |  |  |  |  | Hydrogen bond intensity |  |  |  |  |  | WH |
| P | I |  | t | TCI (A1372/A2900) |  |  |  |  |  |  |  |  |  | LOI (A1429/A893) |  |  |  |  |  | HBI (A3400/A1320) |  |  |  |  |  |  |
| 0.5 | 25 |  | 15 | 0.71 |  |  |  |  | 0.47 |  | 0.24 |  |  | 0.57 | 0.41 |  |  | 0.16 |  | 3.23 |  | 1.67 |  |  | 1.56 | 12.60 |
| Process parameters |  |  |  | Physical and Chemical analysis |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| P |  | I | t | WH (cm) |  | Intensity of C=O stretching |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Aldehyde |  |  |  |  |  |  |  |  |  |  |  |  | Acid |  |  |  |  |  |  |  |
|  |  |  |  |  |  | BT |  |  |  |  |  |  | AT |  |  |  |  |  | BT |  |  |  | AT |  |  |  |
|  |  |  |  |  |  | WN (cm-1) |  |  |  | Intensity |  |  | WN (cm-1) |  |  | Intensity |  |  | WN (cm-1) |  | Intensity |  | WN (cm-1) |  |  | Intensity |
| 0.5 |  | 25 | 15 | 12.60 |  | 0.3364 |  |  |  | 1741 |  |  | 6.91E-3 |  |  | 1756 1750 1742 1730 |  |  | 0.01772 0.01953 0.04016 0.03246 |  | 1728 1720 1710 |  | 4.55E-3 2.29E-3 2.42E-3 |  |  | 1720 1712 |

Table 3 Lattice parameters of control and DC air plasma 
(optimised process parameters) treated sample

| Parameters | Literature | Control | DC air plasma treated sample |
| --- | --- | --- | --- |
| a (Å) | 8.201 | 7.73 | 8.14 |
| b (Å) | 10.380 | 10.23 | 10.44 |
| c (Å) | 7.784 | 7.69 | 7.93 |
| β (º) | 96.5 | 94.5 | 96.2 |
| Crystallinity index |  | 85.8% | 75.8% |

Table 4 Mean pore radius of control and DC air plasma 
(optimised process parameters) treated sample

| Sample | Mean pore radius (m) |
| --- | --- |
| Control (untreated) | 0.117 |
| DC plasma treated sample | 0.336 |

Table 5 Ageing analysis of DC air plasma treated cotton cellulose

| Sample | DC Plasma Treatment |  |  |  |
| --- | --- | --- | --- | --- |
|  | WH (cm) | Carboxyl content | Absorbance ratio | Intensity of Ring CH stretching |
| Control | 9.20 | 1.561 | 1.698 | 1.200E-3 |
| On the day of plasma treatment | 12.60 | 1.613 | 1.817 | 5.395E-4 |
| One week after ageing period | 11.90 | 1.701 | 1.976 | 1.078E-3 |
| One month after ageing period | 10.80 | 2.137 | 2.085 | 6.144E-4 |